## Slide 1
31/08/2016
5622 GaAs and 5629 GaAs growth
5622 GaAs, 08.07.2016
  Wet etch process flow to create hole pattern
  PMMA resist for e-beam
  ALD oxide 25 nm
5629 GaAs, 30.08.2016
  Dry etch process flow to create hole pattern
  ZEP resist for e-beam
  ALD oxide 25 nm

## Slide 2
5622 GaAs
No nanowire growth  due to not completely open holes (15 nm depth of holes is below 25 nm SiO2 film)
Large Poly GaAs crystals
Triangles on the surface of SiO2  effect of high temperature?

## Slide 3
2. 5629 GaAs
Nanowire growth only in one square (Diam 100, Pitch 300)
Length – 2-4 um, diameter 100 nm
Still a lot of poly GaAs, one square is fully covered by GaAs (Diam 150, Pitch 300)
Triangles on the surface of SiO2  effect of high temperature?  increase of SiO2 thickness for next samples
top
Bird eye
Bird eye
Bird eye

## Slide 4
Conclusions
Dry etch process flow works fine to create the holes, confirmed by the grown nanowires
Increase SiO2 to 30 nm  done for next 2 wafers
Next steps
Another sample with the same process flow as 5629 is ready for the growth
2 GaAs wafers are ready for etching step to produce holes. Will be ready by next week (12 samples)